PART 1	GENERAL

1.1	SUMMARY

- Provide all equipment and materials, and do all work necessary to furnish and install the Rollaway “H” Style Football Goal, as indicated on the drawings and as specified herein.

1.2	RELATED WORK

- Examine Contract Documents for requirements that affect work of this section.  Other specification sections that directly relate to work of this Section include, but are not limited to:

  - Section 02200 - Earthwork; Excavation and Backfill and establishment of subgrade elevations.

  - Section 02511 - Asphalt Concrete Pavement

  - Section 02535 - Synthetic Track Surfacing

  - Section 02542 - Synthetic Field Surfacing

  - Section 03300 - Cast-in-Place Concrete; Concrete foundations and bases for goals.

1.3		REFERENCES

- Comply with applicable requirements of the following standards.  Where these standards conflict with other specified requirements, the most restrictive requirements shall govern.

      - U.S. Tennis Court and Track Builders Association

      - National Federation of State High School Associations (NFSHSA)

      - National Collegiate Athletic Association (NCAA)

      - International Amateur Athletic Foundation (I.A.A.F.)

      - Manufacturers Data and Recommended Installation Requirements.

1.4		SUBMITTALS

- Manufacturers Product Data

            - Provide manufacturer’s product literature, technical specifications and other data prior to actual field installation work for Architect or Owner’s Representative review.

# Shop Drawings

  - Provide drawings of manufacturers recommended installation and foundation requirements prior to actual field installation work for Architect or Owner’s Representative review.

1.5		QUALITY ASSURANCE

- Manufacturers warranties shall pass to the Owner and certification made that the product materials meet all applicable grade trademarks or conform to industry standards and inspection requirements.

1.6	DELIVERY, STORAGE AND HANDLING

- Materials delivered to the site shall be examined for concealed damage or defects in shipping. Any defects shall be noted and reported to the Owner’s Representative.

- Replacements, if necessary, shall be immediately re-ordered, so as to minimize any conflict with the construction schedule.

- Sound materials shall be stored above the ground under protective cover or indoors so as to provide proper protection.

PART 2	PRODUCTS

2.1		MANUFACTURERS

- Manufacturers and product selections named are provided to establish the minimum standard.

      - Rollaway “H” Style Football Goal Post - As manufactured by AAE (Aluminum Athletic Equipment Co.); 1000 Enterprise Drive, Royersford, PA 19468; Toll Free (800) 523-5471.

2.2		Rollaway “H” Style Football Goal

- RHG Model - Shall be as manufactured by AAE:

  - Model # RHG-HS (High School Model), Uprights: (two) 4"dia. x .125"wall x 24'0"long, 6061T6 mill finish aluminum uprights with 14'0'' height above the crossbar, welded stay connectors and welded aluminum top cap with flag attachment; Crossbar: (one) 4"dia. x .125"wall, 6061T6 mill finish aluminum crossbar 22'4"; Rear Ground Bar: (one) 4"dia. x .226"wall x  24'0"long, 6061T6 aluminum tube with welded corners and reinforced gussets; Side Ground Bar: (two) 4"dia. x .226"wall x  13'0"long 6061T6 aluminum tube; Wheels: (two) dual rollaway pneumatic wheels for each upright w/ stainless steel axle; Hardware: All stainless steel and galvanized hardware. Includes: Model No. WDF - Wind Directional Flag: two-ply nylon flag streamer 4" x 42" high visibility red

  - Model # RHG-NCAA (Collegiate Model), Uprights: (two) 4"dia. x .125"wall x 30'0"long, 6061T6 mill finish aluminum uprights with 20'0'' height above the crossbar, welded stay connectors and welded aluminum top cap with flag attachment; Crossbar: (one) 4"dia. x .125"wall, 6061T6 mill finish fully welded aluminum crossbar 17'6"; Rear Ground Bar: (one) 4"dia. x .226"wall x  19'2"long, 6061T6 aluminum tube with welded corners and reinforced gussets; Side Ground Bar: (two) 4"dia. x .226"wall x  15'0"long 6061T6 aluminum tube; Wheels: (two) dual rollaway pneumatic wheels for each upright w/ stainless steel axle; Hardware: All stainless steel and galvanized hardware. Includes: Model No. WDF - Wind Directional Flag: two-ply nylon flag streamer 4" x 42" high visibility red

  - Model # RHG-PRO (Professional Model), Uprights: (two) 4”dia. x .125” wall x 30’0” long, 6061T6 mill finish aluminum uprights with 20’0” height above the crossbar, welded stay connectors and welded aluminum top cap with flag attachment; Crossbar: (one) 4”dia. x .125”wall, 6061T6 mill finish fully welded aluminum crossbar 17’6”; Rear Ground Bar: (one) 4”dia. x .226”wall x 19’2” long, 6061T6 aluminum tube with welded corners and reinforced gussets; Side Ground Bar: (two) 4”dia. x .226”wall x 15’0” long 6061T6 aluminum tube; Wheels: (two) double 12” diameter pneumatic tires with 3/4” diameter stainless steel axle, flip to engage wheels; Hardware: All stainless steel and galvanized hardware. Includes: Model No. WDF – Wind Directional Flag: two-ply nylon flag streamer 4” x 42” high visibility red

  - Model # RHG-PRO/9 (Professional Model/9’), Uprights: (two) 4”dia. x .125” wall x 30’0” long, 6061T6 mill finish aluminum uprights with 20’0” height above the crossbar, welded stay connectors and welded aluminum top cap with flag attachment; Crossbar: (one) 4”dia. x .125” wall, 6061T6 mill finish fully welded aluminum crossbar 8’0” long; Rear Ground Bar: (one) 4”dia. x .226”wall x 9’8” long, 6061T6 aluminum tube with welded corners and reinforced gussets; Side Ground Bar: (two) 4”dia. x .226”wall x 13’0” long 6061T6 aluminum tube; Wheels: (two) double 12” diameter pneumatic tires with 3/4” diameter stainless steel axle, flip to engage wheels; Hardware: All stainless steel and galvanized hardware. Includes: Model No. WDF – Wind Directional Flag: two-ply nylon flag streamer 4” x 42” high visibility red

  - Model # RHG-NFL-35 (NFL Model), Bottom Uprights: (two) 4”dia. x .125” wall x 11’0” long, 6061T6 mill finish aluminum, welded aluminum 3.7”dia. x .25” wall x 15’0” long aluminum insert, welded stay connectors for crossbar attachment; Top Uprights: (two) 4”dia. x .125” wall x 35’0” long, 6061T6 mill finish aluminum uprights with 35’0” height above the crossbar, welded aluminum top cap with flag attachment; Crossbar: (one) 4”dia. x .125” wall, 6061T6 mill finish fully welded aluminum crossbar 17’6” long; Rear Ground Bar: (one) 4”dia. x .226” wall x 19’2” long, 6061T6 aluminum tube with welded corners and reinforced gussets; Side Ground Bar: (two) 4”dia. x .226”wall x 15’0” long 6061T6 aluminum tube; Wheels: (two) double 12” diameter pneumatic tires with 3/4” diameter stainless steel axle, flip to engage wheels and dual rollaway pneumatic wheels for each upright w/ stainless steel axle; Hardware: All stainless steel and galvanized hardware. Includes: Model No. WDF – Wind Directional Flag: two-ply nylon flag streamer 4” x 42” high visibility red

  - Model # RHG-NFL-35/9 (NFL Model/9’), Bottom Uprights: (two) 4”dia. x .125” wall x 11’0” long, 6061T6 mill finish aluminum, welded aluminum 3.7”dia. x .25” wall x 15’0” long aluminum insert, welded stay connectors for crossbar attachment; Top Uprights: (two) 4”dia. x .125” wall x 35’0” long, 6061T6 mill finish aluminum uprights with 35’0” height above the crossbar, welded aluminum top cap with flag attachment; Crossbar: (one) 4”dia. x .125” wall, 6061T6 mill finish fully welded aluminum crossbar 8’0” long; Rear Ground Bar: (one) 4”dia. x .226”wall x 9’8” long, 6061T6 aluminum tube with welded corners and reinforced gussets; Side Ground Bar: (two) 4”dia. x .226”wall x 13’0” long 6061T6 aluminum tube; Wheels: (two) double 12” diameter pneumatic tires with 3/4” diameter stainless steel axle, flip to engage wheels and dual rollaway pneumatic wheels for each upright w/ stainless steel axle; Hardware: All stainless steel and galvanized hardware. Includes: Model No. WDF – Wind Directional Flag: two-ply nylon flag streamer 4” x 42” high visibility red

### Accessories

- Model # GW-95, Ground Bar Weight: ninety-five pound steel weight encased in a 4" square aluminum tube with welded endcaps and brackets to add additional counter balance weight in anchoring goal; completely rust-proof

- Model # GP-4R, 4" thick foam encased in 18 oz. double knife-coated vinyl, Velcro closure in rear, school name or logos available; specify color

- Model # RHG-HMK, 2” x 2” x 1/4” thick steel angles welded together with a 5” x 1/4” thick steel flat plate in the middle to form a “C-channel” with a welded 3” sq. steel hitch receptacle, vinyl-coated black

- Model # RHG-RWD, double 12” diameter pneumatic tires with 3/4” diameter stainless steel axle, flip to engage wheels, vinyl coated yellow

PART 3	EXECUTION

3.1  		INSPECTION

- Examine the areas and conditions where equipment and systems are to be installed and notify the contractor of conditions detrimental to the proper and timely installation and completion of the work.

- Do not proceed with the work until unsatisfactory conditions have been corrected by the contractor in a manner acceptable and to the satisfaction of the Architect/Engineer or Owner's Representative.

3.2	INSTALLATION

- All athletic equipment shall be installed as indicated on approved submittals as recommended and in strict accordance with manufacturer's written directions and as indicated on the drawings and specified herein.

- All concrete footings for athletic equipment shall be installed as indicated on the drawings and in accordance with Section 03300, Cast-in-Place Concrete.

- All sleeves required for athletic equipment installation shall be set plumb and true to line and grade in concrete as indicated on the drawings and per manufacturer's recommendation.

- All athletic equipment shall be installed in strict accordance with the latest rules, regulations and specifications governing that sport or event for which it is being installed.

3.3  		TESTING, ADJUSTMENT AND OPERATION

- All athletic equipment requiring testing, adjustments and operation shall be tested for proper operation and adjusted to conform to specified standards.

- Provide certifications as required, indicating that equipment has been tested and adjusted to conform to specified standards.

- Provide operating and maintenance instructions and manuals to Owner -designated personnel for the proper operation and care of equipment after equipment has been tested and adjusted to conform to specified standards.

3.4  		CLEANING

- Upon completion of work in any given area, remove all trash and debris from the work area and leave in clean condition.

- END OF SECTION -